## Slide 1: MPC - MEAM Parameter Calibration Tool

## Slide 2: Motivation
To build the entire atomic scale platform from the electronic scale and experimental data.
  Material properties are calculated at the electronic and atomistic scales, for efficient handshakes
To reduce the learning curve in using the electronic and atomic scales
  A teaching tool

## Slide 3
MEAM Parameter Calibration (MPC) tool for elements and alloys
Outputs:
- *.library.meam
- *.parameter.meam
- plot data (CSV)
- restart data
- template for
calibration targets
lammps.sandia.gov
R.L. Carino
Model Calibration Wrapper (MATLAB)*
C.D. Barrett
lammps_MPC
(C, MATLAB)
LAMMPS+MEAM
(C++, Fortran)
Material Properties Calculator GUI (MATLAB)*
Material Properties Repository
Material Properties Calculator
(MATLAB)*
VASP DFT
(Fortran)
VASP (proprietary)
Experimental Data
* in development
Calibration targets

## Slide 4: Currently supported calibration targets
Single elements
  Energy-Volume curves
  Elastic constants
  Vacancy energy
  Interstitial energy
  Surface energy
  Generalized stacking fault energy
Binaries
  Binary lattices heat of formation
  Binary lattices elastic constants
  Replacement substitution energy
  Foreign element interstitial energy
Ternaries
  Binding energies
Notes: D. SINGLE ELEMENT CACULATIONS
1. Left-click LIBRARY popup to select the element
2. Right-click LIBRARY popup, then select 'RUN ALL calculations ...', or
'RUN CHECKED calculations ...' if there are checked items.
Selecting a calculation will toggle its check mark. The 'Primary EV Curve Calculation'
will be automatically performed if it is required but not selected.
The text display and the plot area will show the results of the calculations.
To switch plots between the EVs and GSFEs, click the left popup below the text display
area, select either EVs or GSFEs, then click the 'Plot' button.
If the menu item 'File | Write plot data to file' is checked, then the plotted points
will be written as comma-separated-values (CSV) to the 'plots' subdirectory
(for examples: Al-EVs.CSV, Al-GSFEs.CSV).
E. BINARY CACULATIONS
1. Left-click LIBRARY popup to select the binary
2. Right-click LIBRARY popup to SELECT binary lattice(s). In the resulting dialog, to
select multiple lattices, hold down the 'Ctrl' key then click on the desired lattices.
3. Right-click LIBRARY popup, then select 'RUN ALL calculations ...', or
'RUN CHECKED calculations ...' if there are checked items.
Selecting a calculation will toggle its check mark. The 'Binary EV Curve Calculation'
will be automatically performed if it is required but not selected.
The text display and the plot area will show the results of the calculations.
To show other plots of data generated by the binary calculations, select the data for the
y- and x-axes using the popups on the left of the 'Plot' button, then click 'Plot'.
If the menu item 'File | Write plot data to file' is checked, then the plotted points
will be written as comma-separated-values (CSV) to the 'plots' subdirectory.
The file name is composed from the tag(s) for the computation (ex. E0, E1, H, Nx, C11,
Substitution, H_vs_Nx) and the tag for the element or binary (ex. Al, Al+Mg).
F. TERNARY CACULATION
1. Left-click LIBRARY popup to select the ternary
2. Right-click LIBRARY popup, then select 'Run Binding Energy calculations ...'
The text display and the plot area will show the results of the calculations.
To show other plots of data generated by the binding energy calculations, select the data
for the y- and x-axes using the popups on the left of the 'Plot' button, then click 'Plot'.
If the menu item 'File | Write plot data to file' is checked, then the plotted points
will be written as comma-separated-values (CSV) to the 'plots' subdirectory.

## Slide 5: Possible future validation calculations in MPC
Phase diagrams (binary and ternary)
Thermal expansion coefficients and specific heats
Generalized interfacial fault energies (grain boundary defect validation)
Surface atom absorption energies
Solute effects on slip and twinning
Vacancy migration and diffusion energies

## Slide 6
*.library.meam
*.parameter.meam
Good
fit ?
Yes
Generate candidate MEAM parameters
No
LAMMPS
+
MEAM
lammps_MPC()
lammps_extract()
*.library.meam
*.parameter.meam
*.atoms.data
lammps_cmd()
EV
Elastics
Vacancy
Substitution
Interstitial
Surface
GSF
Binding
*.library.meam
*.parameter.meam
Optimizer
Calibration targets:
DFT; experiments
Initial
*.library.meam
*.parameter.meam
MEAM parameter fitting strategy
User inputs
Material Properties Repository

## Slide 7: User interface
*.library.meam
*.parameter.meam
Plots
Plot controls
Calibration controls
Text display
Notes: A. OVERVIEW
1. What is implemented in this version?
- LAMMPS is invoked as a library, not as an external process
- load MEAM library file
- select an element from library, or more if working with an alloy
- specify primary, secondary 1, secondary 2 structures for an element/component
- load MEAM parameter file
- edit library entries, parameter file entries
- run one or more LAMMPS calculations for a single element
. Primary EV curve
. Secondary EV curve
. Secondary2 EV curve
. Elastic Constants Calculation
. Vacancy Energy Calculation
. Interstitial Energy Calculations
. Surface Energy Calculations
. Generalized Stacking Fault Energy (GSFE) Calculations
- plot single element EV curves, GSFE curve(s)
- specify one or more binary structures
- run one or more LAMMPS calculations for one of more binaries
. Binary EV Curves
. Binary Elastic Constants Calculation
. Substitution Energy
. Interstitial Substitution Energy
- plot results of binary calculations
- run binding energy calculation for a ternary
- plot results of ternary calculations
- specify calibration target data for each LAMMPS calculation enumerated above
- select library file entries associated with elements as calibration parameters
- select parameter file entries associated with elements, binaries and ternaries
as calibration parameters
- attempt to automatically fit the selected calibration parameters so that the
results of the LAMMPS calculations will approach the calibration targets
within specified tolerances
- recall/redisplay results of attempted fits
- write MEAM library file, MEAM parameter file, MPCv4 restart file
- write plot data to file
- write file templates of calibration target data for single element, binary, ternary
- write LAMMPS output log to file, or 'none'

## Slide 8: Workflow
Load MEAM library file
Select an element or the components of an alloy
Load MEAM parameter file
Specify the Primary, Secondary 1, Secondary 2 structures for the MEAM elements
Edit MEAM parameters (library or parameter file entries)
Test-run LAMMPS calculations
Calibrate parameters
Write results to files
Notes: C. SEQUENCE OF OPERATION
Most actions are specified using point-and-click. The text display gives a summary of the
effect of the most recent action.
1. Load MEAM library file
The file library.meam from the LAMMPS distribution is automatically loaded upon start up
if the file is found in C:\MPCv4\examples. Click menu item File | MEAM library file
to reload it or to load another library file.
2. Select an element or the components of an alloy.
1. Left-click LIBRARY popup to select an element. The library entries for the element will
display, but are not editable (yet).
2. Right-click LIBRARY popup then select 'Add ...' to add as MEAM element
3. Repeat 2.1 and 2.2 if working with an alloy
4. To remove an element that was 'Add ..'ed, select it as in 2.1, then right-click as in 2.2,
but select 'Delete ...'
5. After selecting the desired element or alloy components, right-click LIBRARY popup,
then select 'Fix ...'. This wil fix the element or alloy components.
3. Load a MEAM parameter file
Click menu item File | MEAM parameter file to load (or reload) a MEAM parameter file.
4. Specify the Primary, Secondary 1, and Secondary 2 structures for the MEAM elements
1. Left-click LIBRARY popup to select the element
2. Right-click LIBRARY popup, then select 'Primary structure ...'. In the list dialog
that appears, select a structure, then 'OK'.
3. Repeat 4.2 for the Secondary 1 and Secondary 2 structures
4. Repeat from 4.1 for each MEAM element.
5. Edit MEAM parameters
LIBRARY entries (if enabled), and non-indexed PARAMETERS entries (rc, delr, etc) may be
edited directly.
For indexed PARAMETERS entries, select an element, a binary, or a ternary to display its
associated parameter file entries. Then right-click the entry and select a possible
action: 'Add ...', 'Edit ...', 'Delete ...'
If a MEAM parameter is changed, the results of previous calculations (if any) are invalidated.
6. Test-run LAMMPS calculations (see section D, E, F, below)
7. Calibration (see section G below)
8. Write results to files
- MEAM library & parameter files: File | Write library and parameter files
- MPCv4 restart data: File | Write restart file (can be loaded using File | Load restart file)
- Plot data: File | Write plot data to file (must be checked; uncheck to cancel)
- Templates for calibration target data: File | Write calibration data template
(must be checked; uncheck to cancel)
- LAMMPS output log: File | Re-open LAMMPS, specify '-log' for Argument #1, and the file
name for the Argument #2 (or 'none' to prevent creation of log)

## Slide 9: Parameter fitting
Do steps 1-6 of ‘Workflow’. Initialize all desired calibration parameters
Create file templates for calibration targets
Edit+rename templates to specify actual targets
Load calibration targets
Select MEAM parameters to calibrate (associated with elements)
Select MEAM parameters to calibrate (associated with binaries, ternaries)
Select calibration targets
Click Calibration ‘Run’. Iterate from Step 5.
Click ‘History’ to redisplay attempted fits.
Notes: G. MEAM Parameter Calibration
1. Perform Section C, steps 1-6. Initialize all MEAM parameter file entries that
will be used as calibration parameters.
2. Create templates for calibration targets as follows:
2.1 Set menu item 'File | Write calibration data template' to be checked.
2.2 Test-run all calculations with the initial MEAM library file and MEAM parameter file
entries. See section D, E, and F above.
2.3 Uncheck menu item 'File | Write calibration data template'.
3. Edit+rename calibration data templates to specify actual calibration targets. Remove or
comment out entries for which no calibration targets are available.
4. Load calibration target data.
4.1 Left-click PARAMETERS popup to select an element, or a binary, or ternary with
calibration data.
4.2 Right-click PARAMETERS popup, select 'LOAD calibration data from file'. Navigate to
a calibration data file made in Step 3.
Alternatively, select an unchecked specific result (E0, E1, Cij, H, Nx, etc) to initiate
a dialog to enter its calibration data.
4.3 Repeat Steps 4.1 and 4.2 for each element/binary/ternary with available calibration data.
5. Select MEAM parameters to calibrate (parameters associated with elements).
5.1 Left-click LIBRARY popup to display an element for which a library file entry is a
MEAM parameter to be calibrated.
5.2 Right-click the label of the library file entry, and select 'Add to calibration parameter list'.
The entry should be included in the 'Parameters= {...}' list below the text display area.
5.3 Repeat Step 5.2 for each library file entry of the selected element that is be included
in the 'Parameters= {...}' list.
5.4 For a parameter file entry associated with the element that is a MEAM parameter to be calibrated,
right-click the entry and select 'Add to calibration parameter list'.
5.5 Repeat from Step 5.1 for each element that has a library file entry be included in the
'Parameters= {...}' list.
6. Select MEAM parameters to calibrate (parameters associated with binaries/ternaries).
6.1 Left-click LIBRARY popup to display binary/ternary for which a parameter file entry is a
MEAM parameter to be calibrated.
6.2 Right-click the parameter file entry, and select 'Add to calibration parameter list'.
The entry should be included in the 'Parameters= {...}' list below the text display area.
6.3 Repeat Step 6.2 for each parameter file entry of the selected binary/ternary that
is be included in the 'Parameters= {...}' list.
6.4 Repeat from Step 6.1 for each binary/ternary that has a parameter file entry be included in the
'Parameters= {...}' list.
7. Select calibration targets.
7.1 Left-click LIBRARY popup to display an element, a binary, or a ternary with calibration data
to be used as calibration target.
7.2 Right-click PARAMETERS popup, select an unchecked 'Scalar: ...' or 'Curve: ...'. If the latter,
a dialog will accept inputs of the left and right indices of the data points in the curve to be
used as calibration targets. If targetting the minimum in the curve, enter the suggested index
of the minimum point for the left and right indices. The selected target should be included in
the 'Targets= {...}' list below the text display area.
7.3 Repeat from Step 7.1 for each element, binary, ternary with calibration data be included in
the 'Targets= {...}' list.
8. Remove calibration targets and/or parameters.
8.1 To remove a library file entry, left-click LIBRARY popup to select the element. Right-click
the label of the library file entry, then select 'Remove from calibration parameter list'.
8.2 To remove a parameter file entry, left-click LIBRARY popup to select the element/binary/ternary.
Right-click the parameter file entry, then select 'Remove from calibration parameter list'.
8.3 To clear the 'Parameters= {...}' and 'Targets= {...}' lists, right-click 'Calibration' label
and select 'Clear calibration targets and parameters'.
9. Click Calibration 'Run'. Wait a few minutes/hours. If bored, click 'Stop'. Try again from Step 5.
10. Click 'History' popup to redisplay attempted fits. Right-click popup to select attempted fits
to delete.